## Slide 1
Hosting institutions

## Slide 2
Anne-Marie Valente-Feliciano
Superconducting RF Cavities for Particle Accelerators

## Slide 3
OUTLINE
Introduction to RF Cavities
Normal-conductors
Superconductors
Surface impedance
    Two-fluid model and BCS theory
Residual resistance
Superheating field
Field dependence of the surface resistance due to thermal feedback
Design Considerations
Example of SRF Cavities
SRF Cavities, A-M Valente-Feliciano, 6 May 2023

## Slide 4: TECHNICAL MOTIVATION FOR SUPERCONDUCTING RF CAVITIES
The principle motivations for using superconducting RF cavities, are:
          High duty cycle or cw operation.
SRF cavities allow the excitation of high electromagnetic fields at high duty cycle, or even cw, in such regimes that a copper cavity's electrical loss could melt the copper, even with robust water cooling.

## Slide 5: SRF Cavities
Large variety, depending on:
  Type of accelerator
  Particle velocity
  Current and Duty factor
  Gradient
  Acceleration or deflecting mode
Modern SRF cavities cover wide range of particles beta (0.05..1),
operating frequencies (0.072..4 GHz) and beam currents (1mA..100mA, CW & Pulsed)

## Slide 6: RF Cavities
Space enclosed by conducting walls that can sustain an infinite number of resonant electromagnetic modes
Shape is selected so that a particular mode can efficiently transfer its energy to a charged particle
An isolated mode can be modeled by an LRC circuit
Lorentz force
An accelerating cavity needs to provide an electric field (E) longitudinal with the velocity of the particle
Magnetic fields (H) provide deflection but no acceleration

## Slide 7: RF Cavities
Devices that store e.m. energy and transfer it to a charged particle beam
  enclosed by conducting walls that can sustain an infinite number of resonant electromagnetic modes
E.m. field in the cavity is solution to the wave equation
Solutions are two family of modes with different eigenfrequencies
  TEmnp modes have only transverse electric fields
  TMmnp modes have only transverse magnetic fields (but longitudinal component for E)
Accelerating mode: TM010
Example: 2 GHz cavity and speed of light e-  L = 7.5 cm, R = 5.7 cm
E
H
H
E
r
f
z
q
E1
q
E2
L = bcTRF/2

## Slide 8: Figures of merit (1)
What is the energy gained by the particle?
Let’s assume a relativistic e-
Integrate the E-field at the particle position as it traverses the cavity
We can define the accelerating field as:
Important for the cavity performance are the ratios of the peak surface fields to the Eacc. Ideally, these should be small to limit losses and other troubles at high fields

## Slide 9: Figures of merit (2)
The power dissipated in the cavity wall due to Joule heating is given by:
The energy stored in the cavity is given by:
The cavity quality factor is defined as:
Dw
0
dv
= G
  Independent of size and material
  Depends only on shape of cavity and electromagnetic mode
very useful for comparing different cavity shapes.
Geometry Factor
Notes: Breit-Wigner function

## Slide 10: SRF cavity performance – Q vs. Eacc
T=2.0 K
f = 1.3 GHz
F. Furuta et al., Proc. EPAC’06, p. 750
Bp  185 mT
Rs  8 nW

## Slide 11: Surface Impedance
The electromagnetic response of a metal, whether normal or superconducting, is described by a complex surface impedance:
surface resistance
surface reactance
For a good conductor and w < ~1016 Hz
The impedance of vacuum is:
For accelerator applications, the rate of oscillation of the e.m. field falls in the radio-frequency (RF) range
(3 kHz – 300 GHz)
Notes: Ratio of electric field at the surface to the total current flowing across a unit line in the surface.

## Slide 12: Electrodynamics of normal conductors
From Drude’s model (“nearly free electrons”), macroscopic phenomenology :
Maxwell’s equations
(linear and isotropic) material’s equations
s
t = l/vF  10-14 s is the electrons’ scattering time
wt << 1 at RF frequencies
Ohm’s law, local relation between J and E
Electrical conductivity 𝜎
Electrons in real metals show Ohmic loss
Imperfections causes local scattering

## Slide 13: Surface impedance of normal conductors
From previous slide you obtain:
skin depth:
Solution (semi-infinite slab):
Hy(x,t)
Ez(x,t)
x
z
y
Example: Cu at 1.5 GHz, 300 K (s = 5.8107 1/Wm, m0=1.2610-6 Vs/Am, m=1)
d = 1.7 mm, Rs = 10 mW

## Slide 14: What happens at low temperature?
s(T) increases, d decreases The skin depth (the distance over which fields vary) can become less than the mean free path of the electrons (the distance they travel before being scattered)
Introduce a new relationship where J is related to E over a volume of the size of the mean free path (l)
Effective conductivity
= t
Contrary to the DC case higher purity (longer l) does not increase the conductivity  anomalous skin effect

## Slide 15: So, how good is Cu at low T?
“Extreme” anomalous limit (OK for Cu in RF and low T)
for Cu
Does not compensate for the refrigerator efficiency!!!

## Slide 16: Superconductivity - reminder
The 3 Hallmarks of Superconductivity

## Slide 17: London equations - Reminder
E=0: Js goes on forever
E is required to maintain an AC current
B is the source of Js
Spontaneus flux exclusion

## Slide 18
Enter RF Superconductivity

## Slide 19: RF Superconductivity
Superconducting electrons are paired in a coherent quantum state, for DC resistivity disappears bellow the critical field.
In RF, there is the BCS resistivity, arising from the unpaired electrons.
Hc(T)=Hc(0)·[1-(T/Tc)2]
For copper
 = 5.8·107 -1 m-1 so at 1.5 GHz, Rs = 10 m
For superconducting niobium
Rs = RBCS + Rresidul and at 1.8K, 1.5 GHz, RBCS = 6 n Rresidual ~ 1 to 10 n

## Slide 20: RF resistance is non zero
z
x
y
vacuum
surface
Local surface resistance
Superconducting 𝑹𝒔 is small but non zero
𝐸𝑥(𝑧 = 0)
𝐽𝑥(𝑧)
Materials provide boundary conditions with finite power dissipation
So, how does Rs for a superconductor compare to that of a normal conductor?
In AC fields, the time-dependent magnetic field in the penetration depth will generate an electric field:
Because Cooper pairs have inertia (mass=2me) they cannot completely shield nc electrons from this E-field  Rs > 0

## Slide 21: Two-fluid model
Gorter and Casimir (1934) two-fluid model: charge carriers are divided in two subsystems, superconducting carriers of density ns and normal electrons of density nn.
The superconducting carriers are the Cooper pairs (1956) with charge -2e and mass 2m
The normal current Jn and the supercurrent Js are assumed to flow in parallel. Js flows with no resistance.
H0
Vacuum
SC
J = Jn + Js

## Slide 22: Electrodynamics of superconductors (at low field)
London equations:
London penetration depth
Currents and magnetic fields in superconductors can exist only within a layer of thickness lL
Note:
Local condition between current and field. Valid if x0 << lL or l << lL

## Slide 23: Surface impedance of superconductors
Electrodynamics of sc is the same as nc, only that we have to change s  s1 – i s2
= s2
s
Penetration depth:
s1 << s2 for sc at T<<Tc
For Nb, lL = 36 nm, compared to d = 1.7 mm for Cu at 1.5 GHz

## Slide 24: Surface impedance of superconductors
Ls: kinetic inductance
For a sc s1 << s2  y <<1

## Slide 25: Surface resistance of superconductor
Rs  s1  l  longer m.f.p (higher conductivity) of unpaired e- results in higher Rs !
Rs  w2  use low-frequency cavities to reduce power dissipation
Temperature dependence:
Unpaired electrons are created by the thermal breakup of Cooper pairs
ns(T)  1-(T/Tc)4
s1(T)  nn(T)  e-D/kBT
T < Tc/2
Notes: Intuitive explanation: if unpaired electrons have higher conductivity they draw a relatively higher fraction of the total current

## Slide 26: Material purity dependence of Rs
If x0 >> lL and l >> lL, the local relation between current and field is not valid anymore (similarly to anomalous skin effect in normal conductors)
The dependence of the penetration depth on l is approximated as
Pippard (1953):
if l >> x0 (“clean” limit)
if l << x0 (“dirty” limit)
Rs has a minimum for l = x0/2
Optimal
l~ξ0/2

## Slide 27: BCS surface resistance (1)
From BCS theory of sc, Mattis and Bardeen (1958) have derived a non-local equation between the total current density J and the vector potential A
can be converted in a product in Fourier domain:
J(q) = -K(q)A(q)
The surface impedance can be derived in term of the Kernel K(q):
for diffuse scattering of electrons at the metal surface

## Slide 28: BCS surface resistance (2)
There are numerical codes (Halbritter (1970)) to calculate RBCS as a function of w, T and material parameters (x0, lL, Tc, D, l)
For example, check http://www.lepp.cornell.edu/~liepe/webpage/researchsrimp.html
A good approximation of RBCS for T < Tc/2 and w < D/ħ is:
RBCS 
C1 = 2.246
Let’s run some numbers: Nb at 2.0 K, 1.5 GHz  l = 40 nm, sn = 3.3108 1/Wm, D/kBTc = 1.85, Tc = 9.25 K
RBCS  20 nW Xs  0.47 mW
Nb
Cu

## Slide 29: Not so fast…
Refrigeration isn’t free:
Time to celebrate !
Carnot efficiency: hC = 2 K/(300 K – 2 K) = 0.007
Technical efficiency of cryoplant: hT  0.2
Total efficiency: htot  0.0014  1/700
Power reduction from Cu(300K) to Nb(2K) is  103

## Slide 30: SRF Material Requirements
Grain boundaries transparent to high RF screening currents in polycrystalline material.
Minimal degradation of superconducting properties by local chemical non-stoichiometry and precipitation of non-superconducting second phases.
Good formability & sustainability to fabrication/preparation processes
Low surface resistance, including low residual resistance.
Superconducting cavities are dominated by their surface quality (Niobium & other SC)
S-wave Cooper pairing with a full superconducting gap on the entire Fermi surface.
High lower critical magnetic field and superheating magnetic
difficult to reach in real “accelerating cavities” (low T, large scale cavity
fabrication, surface defects,…)
High thermal conductivity.
SRF Cavities, A-M Valente-Feliciano, 6 May 2023

## Slide 31: Various Superconducting materials – only one practical and commonly used
“Superheating” field for niobium at 0 K is 2.4 kGauss
Low surface resistance, including low residual resistance.
S-wave Cooper pairing with a full superconducting gap on the entire Fermi surface.
High lower critical magnetic field Hc1 and superheating magnetic HSH
High thermal conductivity.
Uniform composition, no phase transition in the domain of interest
Very large ξ: makes it less sensitive to small crystalline defects (e.g. GB)
Grain boundaries transparent to high RF screening currents in polycrystalline material.
Minimal degradation of superconducting properties by local chemical non-stoichiometry and precipitation of non-superconducting second phases.
Good formability
Currently Nb provides the best compromise to all requirements.

## Slide 32: Experimental results
Small deviations from BCS theory can be explained by strong coupling effects, anisotropic energy gap in the presence of impurity scattering or by inhomogeneities
Frequency dependence
A. Phillip and J. Halbritter, IEEE Trans. Magn. 19(3) (1983) 999.
RBCS can be optimized by tuning the density of impurities at the cavity surface.
Nb, 4.2 K
Dependence on material purity
C. Benvenuti et al., Physica C 316 (1999) 153.
Nb films sputtered on Cu
By changing the sputtering species, the mean free path was varied
Nb,1.5 GHz, 4.2 K
“clean”
“dirty”

## Slide 33: Residual resistance
Possible contributions to Rres:
Trapped magnetic field
Normal conducting precipitates
Grain boundaries
Interface losses
Subgap states
B. Aune et al., Phys. Rev. STAB 3 (2000) 092001.
Nb, 1.3 GHz
Rs = RBCS(w, T, D, Tc, lL, x0, l) + Rres(?)
2 K
For Nb, Rres (~1-10 nW) dominates Rs at low frequency (f < ~750 MHz) and low temperature (T < ~2.1 K)

## Slide 34: Possible contributions to Rres in Nb (1)
Trapped magnetic field
In technical materials, the Meissner effect is incomplete when cooling below Tc in the presence of a residual magnetic field due to pinning
Fluxoids: normal conducting core of area ~px02 and normal-state surface resistance, Rn
if 100% flux pinning
Rres due to Earth’s field (~500 mG) at 1.5 GHz: ~120 nW (~6RBCS(2K))
Apply magnetic shielding around cavities

## Slide 35: Possible contributions to Rres in Nb (2)
Trapped magnetic field
Including the oscillatory motion of a fluxoid due to the Lorentz force:
In the frequency limit where only the tip of the fluxoid vibrates:
Anisotropy parameter
For Nb: rn~510-10 Wm, Hc=2000 Oe, 2g=1
A. Gurevich and G. Ciovati, Phys. Rev. B. 87, 054502 (2013)
 w2

## Slide 36: Possible contributions to Rres in Nb (3)
Normal conducting precipitates
If the bulk H content in high-purity (RRR~300) Nb is > ~5 wt.ppm, precipitation of normal-conducting NbHx islands occurs at the surface if the cooldown rate is < ~1 K/min in the region 75-150 K
B. Aune et al., Proc. 1990 LINAC Conf. (1990) 253.
Nb cavities are heat treated at 600 – 800 °C in a UHV furnace to degas H

## Slide 37: Possible contributions to Rres in Nb (4)
Grain boundaries
Interface losses
Results are still inconclusive
Results are still inconclusive
Finite density of states at the Fermi level:
Residual resistance (s1 sng/D):
Rres ~10 nW at 1.5 GHz for g/D = 10-3
Subgap states
subgap
states
BCS
Tunneling measurements show that the BCS singularity in the electronic density of states is smeared out and subgap states with finite N(e) appear at energies below ∆.
Phenomenological formula [Dynes (1978)]:
g: damping parameter
A. Gurevich, Rev. Accel. Sci. Tech. 5, 119 (2012)
Notes: Mechanisms for subgap states can be intrinsic such as due to strong impurity scattering or strong electron-phonon coupling or extrinsic such as normalconducting precipitates or trapped vortices

## Slide 38: About HTS…
HTS materials have nodes in the energy gap. This leads to power-law behavior of λ(T) and Rs(T) and high residual losses
LTS
HTS
YBCO
Hein M A 1996 Studies in High Temperature Superconductors vol 18 ed A Narlikar (Nova Science Publishers) pp 141–216
x ~ 1 – 2 nm (<< l)  superconducting pairing is easily disrupted by defects (cracks, grain boundaries)
“Granular” superconductors: high grain boundary resistance contributing to Rres
We are stuck with LHe!

## Slide 39: Surface barrier
Meissner currents push the vortex in the bulk
Attraction to the antivortex image pushes the vortex out
How do vortices get in a superconductor?
Two forces acting on the vortex at the surface:
Vortices have to overcome the surface barrier even at H > Hc1
Surface barrier disappears only at H=Hsh
Surface barrier is reduced by defects
Thermodynamic potential G(b) as a function of the position b:
Hsh

## Slide 40: What is the highest RF field applicable to a superconductor?
Penetration and oscillation of vortices under the RF field gives rise to strong dissipation and the surface resistance of the order of Rs in the normal state
the Meissner state can remain metastable at higher fields, H > Hc1 up to the superheating field Hsh at which the Bean-Livingston surface barrier for penetration of vortices disappears and the Meissner state becomes unstable
Meissner State
Abrikosov Vortex Lattice
T
H
Tc
Hc2(0)
Hc1(0)
Normal State
Type-II SC
Hsh(0)
Hsh is the maximum magnetic field at which a type-II superconductor can remain in a true non-dissipative state not altered by dissipative motion of vortices.
At H = Hsh the screening surface current reaches the depairing value Jd = nseD/pF

## Slide 41: Superheating field: theory
Calculation of Hsh(k) from Ginzburg-Landau theory (TTc) [Matricon and Saint-James (1967) ]:
t
Time evolution of the spatial pattern of the order parameter
in a small region around the boundary where a vortex entrance
is taking place, calculated from time-dependent GL-equations.
A. D. Hernandez and D. Dominguez, Phys. Rev. B 65, 144529 (2002)
Plot from Padamsee

## Slide 42: Superheating field: theory
Weak dependence of Hsh on non-magnetic impurities
Calculation of Hsh(T, l) for k >> 1 from Eilenberger equations (0<T<Tc) [Pei-Jen Lin and Gurevich (2012)]:
a = px0/l
F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
Impurity scattering parameter

## Slide 43: Alternative Materials to Nb
Global surface resistance:
Material | Tc (K) | Hc [T] | Hc1 [mT] | Hc2 [T] | (0) [nm] |  [meV]
Nb | 9.2 | 0.2 | 170 | 0.4 | 40 | 1.5
B0.6K0.4BiO3 | 31 | 0.44 | 30 | 30 | 160 | 4.4
Nb3Sn | 18 | 0.5 | 40 | 30 | 85 | 3.1
NbN | 16.2 | 0.23 | 20 | 15 | 200 | 2.6
MgB2 | 40 | 0.32 | 20-60 | 3.5-60 | 140 | 2.3; 7.1
Ba0.6K0.4Fe2As2 | 38 | 0.5 | 20 | >100 | 200 | >5.2
Example: 4 layers 30 nm thick of Nb3Sn on Nb  Ha up to ~400 mT [~Hsh(Nb3Sn)] with Hi ~ 100 mT << Hsh(Nb)
R0Nb3Sn(2 K)  0.1 RbNb(2 K)  Rs  0.15 Rb

## Slide 44: Superheating field: experimental results
Use high-power (~1 MW) and short (~100 ms) RF pulses to achieve the metastable state before other loss mechanisms kick-in
Nb Hc1
Nb3Sn Hc1
Highest Hp ever measured in CW!!!
T. Hays and H. Padamsee, Proc. 1997 SRF Workshop, Abano Terme, Italy, p. 789 (1997) .
RF magnetic fields higher than Hc1 have been measured in both Nb and Nb3Sn cavities.
However max HRF in Nb3Sn is << predicted Hsh…

## Slide 45: However…
In “real” surfaces, the surface barrier can be easily suppressed locally by “defects” such as roughness or impurities, so that vortices may enter the sc already at HRF  Hc1
Hp  30 mT ~ Hc1
G. Muller et al., Proc. 1996 EPAC, Spain, p. 2085 (1996)
1.5 GHz, Nb3Sn film deposited on Nb

## Slide 46: Multilayer Films
If Hc1 is indeed a major practical limit for RF application of high-k materials, a possible solution consists of S-I-S multilayers [Gurevich (2006)]:
Suppression of vortex penetration due to the enhancement of Hc1 in a thin film with d < 
[Abrikosov, (1964)]
= exp(-Nd/l)
A. Gurevich, Appl. Phys. Lett. 88, 012511 (2006)

## Slide 47: Global thermal instability
The exponential temperature dependence of Rs(T) provides a strong positive feedback between RF Joule power and heat transport to the coolant  thermal instability above the breakdown field Hb
k: thermal conductivity
hK: Kapitza conductance
Uniform thermal breakdown field

## Slide 48: Uniform thermal breakdown field
For 1.5 mm thick Nb on 3 mm thick Copper (hK,Cu=8.4 kW/m2 K, kCu=200 W/m K)
Higher frequencies not only reduce the cavity Q0 ( Rs) but also the breakdown field
m0Hb (mT)
f (GHz)
Nb, 2 K, same parameters as previous slide
In case of multilayers the thermal conductance is:
Nb3Sn coating with Nds = 100 nm, s = 10-2 W/m K
Insulating Al2O3 layers, Ndi = 10 nm, i = 0.3 W/m K
di/i = 1/300(ds/s)  Insulating layers are negligible
d/ = 3Nds/s  TFML adds ~30% to the thermal resistance of the Nb shell
Bsh

## Slide 49: Q0(B0) curve
Because of the Tm(H0) dependence, Rs acquires a H0-dependence
B0 (mT)
Q0
Nb, 2 K, 1.5 GHz, G=280 W, Rs and thermal parameters as in previous slides
Surface treatments
Intrinsic non-linearities

## Slide 50: SRF applications and cavity requirements
The specific application, facility requirements and mode of operation will define the choice of the cavity type, operating frequency, other parameters to optimize.
SRF Cavities, A-M Valente-Feliciano, 6 May 2023
Also New Developments for Accelerators for Societal Needs
- See Kazuya Osaki Lecture, Accelerators for medical and industrial applications

## Slide 51: Design Considerations
Residual resistivity: RactualRBCS+Rresidual
Dependence on field – shape, material, preparation
      “Q slope” Electropolishing, baking
      Field emission- cleanliness, chemical processing
      Thermal conductivity, thermal breakdown – High RRR
Multipacting – cavity shape, cleanliness, processing
Higher Order Modes – loss factor, couplers
Mechanical modes– stiffening, isolation, feedback
SRF cavity is a complicated electro-mechanical assembly and consist of:
bare cavity shell with power and HOM couplers
stiffening elements (ring, bars)
welded LHe vessel
Slow and fast frequency tuners
vacuum ports
The design of SRF cavity requires a complex, self consistent electro-mechanical analysis in order to minimize microphonics and/or Lorentz force detuning phenomena and preserving a good cavity tenability simultaneously !
HWR 162.5 MHz cavity for PIP-II
ILC 1.3 GHz 9-cell cavity
ERL 704 MHz 7-cell cavity

## Slide 52: SRF system design is an intricate process
Pulsed operation
CW operation
High beam current
High beam power
Beam quality (emittance) preservation
Low beam power
Heavy beam loading
Lorentz force detuning
RF power dissipation in cavity walls
Beam stability (HOMs)
Parasitic interactions
(input coupler kick, alignment)
Low Qext
Availability of
high-power RF sources
High Qext, microphonics
Mechanical design
stiffness, vibration modes, tunability, thermal analysis
RF design
frequency & operating temperature choice, optimal gradient, cavity shape optimization,
number of cells, cell-to-cell coupling,
HOM extraction, RF power coupling
Input coupler design
HOM damper design
Tuner design
RF controls
Cryostat design
Cavity design
Machine parameters
Effects/cavity parameters
Cryomodule design
What shall we consider when designing a cavity?
Material (impacts losses and operating gradient)
Frequency (impacts size of the cavity, cost, surface resistance, assembly technique, …)
Number of cells (impacts field flatness, tunability, HOM extraction, linac fill factor, mechanical resonances, …)
Aperture size (impacts beam stability, peak fields, HOM damping, …)
Cavity shape (impacts peak surface fields, power dissipation, multipacting, tunability, …)
…
The cavity design is intimately coupled with that of other cryomodule components.

## Slide 53: RF simulations tools
As the real cavity cannot be modeled analytically, we use computer codes
Electromagnetic field calculations
  Fundamental & High Order Modes spectrum, R/Q, G, fields
    2D simulation tools: SUPERFISH, SLANS/CLANS
    3D simulation tools: CST Microwave Studio, HFSS, Omega3P, Comsol Multiphysics, ANSYS
Multipacting simulations
  Determine the areas and voltage levels prone to multipacting
    CST Particle Studio (Particle In Cell, Tracking), SPARK3D, Track3P, MultiPac, MultP-M
Wakefield simulations
  Wake potential, wake impedance
    CST Microwave Studio, ABCI, ECHO, GdfidL
Mechanical simulations
  Mechanical modes and frequencies, thermal deformations, Lorentz force detuning, mechanical stresses
    ANSYS, Comsol Multiphysics, CST, TEM3P

## Slide 54: Types of SRF cavities
There are two distinct types of superconducting RF cavities.
The first type, elliptical TM-mode cavities, is for accelerating charged particles that move at nearly the speed of light, such as electrons in high- energy linacs or storage rings.
The second type, TEM-mode cavities, is for particles that have velocities v much smaller than the speed of light c (e.g., β = 0.01…0.5, where β = v/c), such as the heavy ions or protons at the early stages of acceleration.
At intermediate velocities, both types of structures could be used, depending on application.
Some practical geometries for different particle velocities
TM cavities
TEM cavities

## Slide 55: Low  Resonators
Quarter Wave
Resonator
Radio Frequency Quadrupole
Elliptical
Split Loop Resonator
Spoke cavity
Multi-spoke
Critical applications:
Heavy ion accelerators, e.g. RIA
High power protons, e.g. SNS, Project-X

## Slide 56: High acceleration gradient
Critical applications:
Linear colliders e.g. ILC
X-ray FELs e.g. DESY XFEL, LCLS-II

## Slide 57: Variety of elliptical cavities
LEP: 352 MHz
CESR: 500 MHz
KEKB: 508 MHz
TRISTAN: 508 MHz
SNS: 805 MHz, β = 0.61 and 0.81
TESLA: 1.3 GHz
CEBAF: 1.5 GHz
Fermilab: 3.9 GHz

## Slide 58: Deflecting Cavities
Critical applications:
Crab crossing (luminosity) e.g. KEK-B, LHC
Short X-ray pulses from light sources

## Slide 59: High current ERL cavities
Multi-ampere current possible in ERL
Critical applications:
High average power FELs (e.g. Jlab)
High brightness light sources (e.g. Cornell)
High luminosity e-P colliders (e.g. eRHIC)

## Slide 60: High current SRF photo-injector
Low emittance at high average current is required for FEL.
The high fields (over 20 MV/m) and large acceleration (2 MV) provide good emittance.
High current (0.5 ampere) is possible thanks to 1 MW power delivered to the beam.
Starting point for ERL’s beam.

## Slide 61: Highlights
Unlike in the DC case, dissipation occurs in SC in RF because of the inertia of Cooper-pairs
The surface resistance can be easily understood in terms of a two-fluid model and is due to the interaction of the E-field (decaying from the surface) with thermally excited normal electrons
Rs = RBCS + Rres
The maximum theoretical RF field on the surface of a SC is the superheating field  thermodynamic critical field
Multilayer films may be a practical way to reach Hsh in SC with higher Tc than Nb
Thermal feedback couples Rs at low field to the breakdown field
Increases quadratically with frequency
Decreases exponentially with temperature
Has a minimum as a function of material purity
Residual DC magnetic field
Normal-conducting precipitates (NbH)
…

## Slide 62: Highlights
Elliptical shape cavities are de facto standard for TM mode SRF structures for high β particle accelerators.
The cavity shape shall be optimized for new accelerators based on the machine requirements. A plethora of computer simulation tools is available for multi-variable optimization.
One should pay careful attention to the cavity interfaces with other components of a cryomodule.
Mechanical aspects of cavity design are very important and should be carefully modeled using appropriate codes.
High purity bulk Nb (RRR > 250), typically in the form of several mm thick sheets, is used for fabricating the majority of SRF cavities nowadays.
The fabrication processes are well understood and developed. Some alternative fabrication techniques are being pursued.
Nb/Cu is used for SRF cavities in several machines, e.g., LEP2, LHC, SOLEIL, HIE-ISOLDE (not covered in this tutorial).
Nb3Sn is a promising material, but still in an early R&D stage and demonstrated fields only up to 25 MV/m.

## Slide 63: Further Remarks
SRF technology applied to accelerators is wonderfully complex
  Inherently multi-disciplinary
  Huge number of coupled parameters – everything matters
  If you like simplicity – find other work
  Remember that cost-effectiveness drives everything
    Research, design, fabrication, processing, maintenance, operation
    Nothing is cheap
    We only do this because there is no better way to meet the need
  Designs build upon previous design and operation experience
  Learn from the insights, successes, and difficulties of others
  Accumulated physical understanding is required for engaging unexpected problems
  Contamination can spoil everything.
  But when it works right, it makes the amazing possible.

## Slide 64
Basic SRF cavity…
Quality factor
Q0 µ G / Rs
G = geometry factor
i.e. Eacc depends on the shape
Surface resistance RS
RS(Nb) ~ 1 nΩ @ 2K
<< Rs(Cu) ~ 100 µΩ
Esurf ~ 106-107 V/m
Jsurf ~ 109-1010 A/m2
Hsurf ~ 100 mT or more
lL ~ 50 nm
Region of highest
magnetic field
Region of highest
electric field

## Slide 65: Acknowledgments
Inspiration and material from earlier lectures from:
Prof. G. Ciovati, Jlab; Prof. A. Gurevich, ODU; Prof. Steven M. Anlage, UMD; Prof. J. Knobloch, BESSY; Prof. H. Padamsee, Cornell U.; S. Belomestnykh, FNAL.
Tutorials on SRF can be found on the webpages of SRF Conferences: http://accelconf.web.cern.ch/accelconf/

## Slide 66: References
Standard textbooks on SRF
  H. Padamsee, J. Knobloch and T. Hays, RF Superconductivity for Accelerators, J. Wiley & Sons, New York, 1998
  H. Padamsee et al “RF superconductivity for accelerators”, 2nd edition, WILEY-VCH (2008)
  H. Padamsee, RF Superconductivity. Science, Technology, and Applications, Wiley-VCH, Weinheim, 2009
Reviews on SRF
  J. P. Turneaure et al “The surface impedance of superconductors and normal conductors: the Mattis-Bardeen theory”, J. Supercond. 4, 341-355 (1991)
  A. Gurevich “Theory of RF superconductivity for resonant cavities”, Supercond. Sci. Technol. 30 034004 (2017)
  CERN Accelerator School – 1955 – 2016 (https://cds.cern.ch/collection/CERN%20Yellow%20Reports?ln=en)
Introduction to solid state physics (before second quantization)
  N. W. Ashcroft and N. D. Mermin, “Solid State Physics” Thomson Learning (1976)
Introduction to superconductivity + minimal knowledge on condensed matter physics (but lack of SRF…)
  S. Fujita and S. Godoy “Quantum statistical theory of superconductivity”, Springer, (1996)
Dictionary of superconductivity
  M. Tinkham “Introduction to superconductivity”, 2nd edition, Dover (2004)
More advanced textbook on superconductivity
  N. Kopnin “Theory of Nonequilibrium Superconductivity”, Oxford Science Publications (2001)

## Slide 67: References
BCS resistance
  J. Bardeen, L. N. Cooper, and J. R. Schrieffer,Phys. Rev.108, 1175 (1957). [Matrix elements for static magnetic field were calculated
here]
  D. C. Mattis and J. Bardeen, Phys. Rev.111,412 (1958). [1st order perturbation of RF response and nonlocality, substituting matrix elements modified for RF]
  J. Halbritter, Z. Physik266, 209 (1974) [Fermi‘s golden rule applied for constant martix element and two fluid approximation ]
  J. Halbritter, KFK-Ext.03/70-06 (1970) [FORTRAN66 code for BCS resistance of f</2 and arbitrary 𝜉0, 𝜆𝐿, 𝑙]
Residual resistance due to flux oscillation
  J. Bardeen and M. J. Stephen, Phys. Rev.140, A1197(1965). [Phenomenological model to describe trapped flux as a string]
  J. I. Gittleman and B. Rosenblum, Phys. Rev. Lett.16,734 (1966). [driven-damped ordinary differential equation for flux oscillation driven by Lorentz force]
  M. Checchin, M. Martinello, A. Grassellino, A. Roma-nenko, and J. F. Zasadzinski, Supercond. Sci. Technol.30, 3 (2017). [application of
Gittleman & Rosenblum for SRF cavities]
  A. Gurevich and G. Ciovati, Phys. Rev. B87, 054502 (2013). [keeping tension term and solved partial differential equation instead]
Quench field
  J. Matricon and D. Saint-James Phys Lett A 24 241 (1967). [solving Ginzburg-Landau equation to estimate superheating field]
  F. P.-J. Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012). [solving Eilenberger equations to estimate superheating field in arbitrary impurity]
  Vudtiwat Ngampruetikorn and J. A. Sauls, Phys. Rev. Research 1, 012015(R) (2019). [including inhomogeneity at the surface]

## Slide 68: BACK-UPS

## Slide 69: Figures of Merit

## Slide 70: Accelerating voltage and transit time
d
Assuming charged particles moving along the cavity axis, one can calculate
accelerating voltage as
For the pillbox cavity we can integrate this analytically:
To get maximum acceleration:
𝑇(,-./&( = 𝑡01&( − 𝑡0.(0,
2
= 𝑇* ⇒ 𝑑 = 𝛽𝜆
2
2 ⇒ 𝑉! = 𝜋 𝐸*𝑑
Thus, for the pillbox cavity T = 2/ .
For efficient acceleration, choose a cavity geometry and a mode where:
  Electric field is along the particle trajectory
  Magnetic field is zero along the particle trajectory
  Velocity of the electromagnetic field is matched to particle velocity
where T is the transit time factor.

## Slide 71: Accelerating Gradient (Eacc)
Accelerating field (gradient) is defined as the voltage gained by a particle divided by a reference length
For velocity of light particles:
N – no. of cells
For less-than-velocity-of-light cavities (β < 1), there is no universally adopted definition of the reference length
However multi-cell elliptical cavities with β < 1
Length per cell
2
d  N
acc
E
d
 Vc
2
d  
Unfortunately, the cavity length is not easy to specify for shapes other than pillbox so usually it is assumed to be d = βλ/2. This works OK for multi-cell cavities, but poorly for single-cell cavities or low β cavities

## Slide 72: Stored energy & quality factor
Energy density in electromagnetic field:
Because of the sinusoidal time dependence and 90° phase shift, the energy oscillates back and forth between the electric and magnetic field. Then the total stored energy in a cavity is given by
or roughly 2π times the number of RF cycles it takes to dissipate the energy stored in the cavity. It is determined by both the material properties and cavity geometry and is ~104 for NC cavities and ~1010 for SC cavities at 2 K.
OP
Recall that the surface resistance is the internal resistance for a unit length and unit width and for NC materials is 𝑅/ = 4 ,
where 𝜎 is the material conductivity and 𝛿 is the skin depth.
We are assuming that the surface resistance Rs does not vary over the cavity surface and has no field dependence.
Measures cavity performance as to how lossy cavity material is for given stored energy
An important figure of merit is the quality factor, which for any resonant system is

## Slide 73: Peak surface fields
Peak surface fields are important for the SRF cavity performance. They should be made as small as possible in ”real” cavities. Pillbox will serve as a reference.
The peak surface electric field is responsible for field emission.
The peak surface magnetic field has fundamental limit: critical field of SC state.
r
R
0
E, H

## Slide 74: Power Dissipation (Pdiss)
Surface current results in power dissipation proportional to the surface resistance (Rs)
Power dissipation per unit area
Total power dissipation in the cavity walls
For superconductors 
  per unit length
  per unit area
For normal conductors 
  per unit length
  per unit area
NC cavities favor high frequencies, SC cavities favor low frequencies.
Frequency dependence
To minimize the losses, one needs to maximize the denominator. By modifying the formula, one can make the denominator material-independent: G⋅R/Q – this new parameter depends only on the cavity geometry and can be used during cavity shape optimization.

## Slide 75: Geometrical Factor (G)
Geometrical factor [Ω]
  Product of the qualify factor (Q0) and the surface resistance (Rs)
  Independent of size and material
  Depends only on shape of cavity and electromagnetic mode
For the pillbox cavity we get G = 257 Ω. If the cavity is made of copper (σ = 5.8×107 S/m) and operates at 1.5 GHz, we get δ = 1.7 μm, Rs = 10 mΩ, and Q0 = G/Rs = 25,700
very useful for comparing different cavity shapes.

## Slide 76: Shunt Impedance (Rsh) and R/Q
Shunt impedance (Rsh) [Ω]
Maximize shunt impedance to get maximum acceleration
Note: Sometimes the shunt impedance is defined as or quoted as impedance per unit length (Ω/m)
A related quantity is the ratio of the shunt impedance to the quality factor, which is independent of the surface resistivity and the cavity size:
R/Q [Ω]: Measures of how much of acceleration for a given power dissipation
Optimization parameter:
R/Q and RshRs
  Independent of size (frequency) and material
  Depends on mode geometry
  Proportional to no. of cells
sh s s
Q Q
R R  Rsh QR  R G
In practice for elliptical cavities
  R/Q ~ 100 Ω per cell
  RshRs ~ 33,000 Ω2 per cell
characterizers losses in a cavity
This parameter is frequently used as a figure of merit and is useful in determining the level of mode excitation by bunches of charged particles passing through the cavity. Sometimes it is called the geometric shunt impedance. For the pillbox cavity R/Q = 196 Ω

## Slide 77: TM010 Mode in a Pill Box Cavity
Energy content
Power dissipation
Geometrical factor
0 0 1 01
2
U E2 J 2 ( x
)LR2
0
1 01
2
P
E 2 Rs
J 2 ( x
)(R L)R
x01
L
G
2 (R L)
2.40483
x01
J1 ( x01 ) 0.51915
Energy Gain
Gradient
Shunt impedance
L
W E0 sin
2
2
2
1 01
1
s
L
Rsh
R 3 J 2 ( x
sin
) R(R L)
0
/2
acc
W
L
E
E 2 sin

## Slide 78: Types of SRF cavities
Cavity families (low-β , middle-β & high-β )

## Slide 79: SRF Cavity Limitations

## Slide 80: Real Performance - Q vs. accelerating field
Magnetic fields of 1.7 kGauss (multi-cell) to 1.9 kGauss (single cell)
Can be achieved, and recently 2.09 kGauss achieved at Cornell.

## Slide 81: Limit on Fields
Field emission – clean assembly
Magnetic field breakdown (ultimate limit) - good welds, reduce surface fields
Thermal conductivity – high RRR material
Local heating due to defects
Fields of 20 to 25 MV/m at Q of over 1010 is routine

## Slide 82: Choice of material and preparation
High “RRR” material (300 and above)
Large grain material is an old “new” approach
Buffered Chemical Polishing (BCP) (HF – HNO3 – H2PO4 , say 1:1:2)
Electropolishing (HF – H2SO4)
UHV baking (~800 ºC)
Low temperature (~120 ºC).
High pressure rinsing
Clean room assembly

## Slide 83: Multipacting
Multipacting is a resonant, low field conduction in vacuum due to secondary emission
Easily avoided in elliptical cavities with clean surfaces
May show up in couplers!
Multipacting in Stanford SCA cavity,
1973 PAC

## Slide 84: Higher Order Modes (HOM)
Energy lost by charge q to cavity modes:
Longitudinal
and Transverse
Energy is transferred from beam to cavity modes
The power can be very high and must be dumped safely
Transverse modes can cause beam breakup
Solution: Strong damping of all HOM,
Remove power from all HOM to loads
Isolated from liquid helium environment.

## Slide 85: Electromechanical issues
Lorentz detuning
Pondermotive instabilities
Pressure and acoustic noise
Solutions include
  broadening resonance curve
  feedback control
  good mechanical design of cavity and cryostat

## Slide 86: Miscellaneous hardware
Fundamental mode couplers
Pick-up couplers
Higher-Order Mode couplers
Cryostats (including magnetic shields, thermal shields)
Helium refrigerators (1 watt at 2 K is ~900 watt from plug)
RF power amplifiers (very large for non energy recovered elements

## Slide 87: Cavity Fabrication & Preparation

## Slide 88: Fabrication and surface preparation steps
The bulk niobium cavities are fabricated by electron beam welding of formed or machined parts.
Typical fabrication and surface processing steps include:
  Surface inspection and cutting niobium sheets of high RRR material.
  Forming half-cells by deep drawing, spinning or hydroforming.
  Forming or machining other parts of the structure: beam pipes, various ports, parts for HOM couplers, etc.
  Mechanical polishing imperfections and dipping in an HCl or H2SO4 bath to eliminate metal impurities; rust checking by dipping overnight in a water bath.
  Light chemical etching
  Electron beam welding sub-assemblies.
  RF testing and tuning of sub-assemblies.
  Mechanical trimming sub-assemblies as necessary.
  Light chemical etching
  Electron beam welding the complete structure from sub-assemblies.
  Cavity inspection, grinding off imperfections on the inner welding seams, where impurities or micro-cracks might be apparent.
  Heavy chemical etching (BCP or EP) to remove the mechanically damaged surface layer and other imperfections.
  High-temperature hydrogen degassing in an all-metal vacuum furnace in a temperature range between 600 and 950◦C
  RF measurements of the cavity frequency. Tuning of the structure to achieve the desired field flatness.
  Final surface preparation (e.g., nitrogen doping, light EP and HPR) before acceptance testing in a vertical dewar.
Typical superconducting RF cavities are made of high purity niobium, either in a bulk form or as a thin layer deposited on the inner surface of copper structure.
To achieve good performance, the high purity of niobium must be maintained throughout the fabrication process.
In addition, the inner surface of the cavity, exposed to strong electromagnetic fields, must be carefully prepared.

## Slide 89: Material inspection
The material must be fully recrystallized, otherwise mechanical properties are affected. Sheet metal forming is sensitive to mechanical properties. In particular, a uniform grain size is essential.
Nb sheets are inspected upon receiving, visually and using eddy-current or SQUID scanning (more sensitive). The basic principle is to detect the alteration of the eddy currents with a double coil sensing probe to identify inclusions and defects embedded under the surface.
Usually, a very small fraction of sheets is rejected at this stage.
Technical Specification to Niobium Sheets for XFEL Cavities
Concentration of impurities in ppm |  |  |  | Mechanical properties | 
Ta | ≤ 500 | H | ≤ 2 | RRR | ≥ 300
W | ≤ 70 | N | ≤ 10 | Grain size | ≈ 50 μm
Ti | ≤ 50 | O | ≤ 10 | Yield strength, σ0.2 | 50 < σ0,2 < 100 N/mm2 (MPa)
Fe | ≤ 30 | C | ≤ 10 | Tensile strength | > 100 N/mm2 (Mpa)
Mo | ≤ 50 |  |  | Elongation at break | 30 %
Ni | ≤ 30 |  |  | Vickers hardness HV 10 | ≤ 60

## Slide 90: Overview of cavity fabrication flow

## Slide 91: Cavity fabrication: forming half-cells
The most common fabrication techniques are deep drawing, hydroforming or spinning half-cells.
Beam pipes and other ports are then fabricated, some parts can be made of a lower grade Nb.
Alternative techniques (not commonly used): hydroforming and spinning an entire cavity out of single sheet or tube.
Deep
drawing
Spinning
Niobium sheet
male die
10 ton
female die
mandrel

## Slide 92: Dumb-bell fabrication steps

## Slide 93: Electron beam welding
After forming and trim machining, the parts are electron beam welded together. Welding must be under vacuum, better than 10-5 Torr. Things to check:
Broad welding seam
Operate with defocused beam
Smooth underbead
Overlap at end of welding to avoid accumulation of impurities
Wait to cool down before opening chamber
Some parts, e.g., flanges, can be brazed to cavity ports.
Microstructure of the EB welding area grain size (50 – 2000) μm

## Slide 94: Cavity welding steps

## Slide 95: Tuning for field flatness
Cavity frequency and field flatness then checked and tuned. Usually, the goal is to achieve 98% field flatness.
Set-up for field profile measurements: a metallic needle or bead is perturbing the RF fields while it is pulled through the cavity along its axis. Due to the volume occupied by the bead, the resonance frequency of an eigenmode j is shifted by
Since the TM010 mode has vanishing magnetic field on axis, we can neglect the first term. Thus, measuring the frequency shift due to the metal bead moving from cell to cell will give us an estimate of the storage energy in each cell.
Then one proceeds with deforming cells until the desired field flatness is achieved. A couple of iterations with an automated tuning machine is sufficient.
Before tuning. FF 65%, slope +28 %
After tuning. FF 98%, slope +0.64 %

## Slide 96: RF measurements
3.9 GHz, 1.3 GHz, 650 MHz dumb-bell measurement fixtures