## Slide 1: A REBCO Bulk Superconducting Undulator for the Microscopic Tomography Beamline at SLS 2.0
Marco Calvi
Insertion Devices for Future Light Sources Workshop (ID25)
31 May 2025 to 1 June 2025 - Taipei World Trade Center

## Slide 2: Overview
Introduction
Results of the short sample experimental campaign:
  Sample preparation
  Magnetic measurements: Field optimisation, CoFe versus Ho poles, FCM Reproducibility, Charging time, Flux creep & flux freezing
The meter-long prototype
  Design
  Status of the production
Conclusions

## Slide 3: The bulk High Temperature Superconducting undulator
Example of field cooling magnetisation
time
T. Kii, et al.: Proc. FEL2006 (2006) p. 653.

## Slide 4: Samples Overview
1st Bulk Sample
6mm gap
Bulk Industrial Sample
4mm gap
Bulk Simplified Sample
2nd Bulk Sample
4mm gap
2019
2023
The baseline Sample
4mm gap
4mm gap
2021

## Slide 5: Industrial Sample
Laser Micro Jet SYNOVA
CH
The HTS crystals are embedded (schrink-fit) into a copper matrix with micro-meter accuracy, to be mechanical and thermally stabilised. An additional Aluminium shrinking cylinder is used to precisely assemble the undulator array (in the picture only a cross section)
EDM Wire Erosion

## Slide 6: The facility
±12T
the solenoid
6

## Slide 7: Cryogenic probe with 5 Hall elements

## Slide 8: Staggered Array With CoFe Poles
With additional ferromagnetic poles
4mm gap
10 mm period

## Slide 10: Experimental results - YBCO from ATZ

## Slide 11: Experimental results - YBCO from ATZ

## Slide 12: Experimental results - YBCO from ATZ
⅓

## Slide 13: 200 bulk simulations
Simulating 200 bulks in 3D requires ~6 hours on a powerful workstation
On the new Merlin7 HPC cluster, this takes ~3 hours
this takes ~0.2 ms

## Slide 14: Single Disk characterisation
The Cu-REBCO disks were individually cooled in 1T magnetic field from room temperature down to LN2 and 2D field mapped, on both sides
1the disk 2pre-cooling 3field Cooling 4flux creep 5disk support 62D field map 7drying

## Slide 15: 2D Field map

## Slide 16: Planar Hybrid: Nippon Steel

## Slide 17: Planar Hybrid: Nippon Steel

## Slide 18: Planar Hybrid: Nippon Steel
gap = 4mm
18

## Slide 19: Impact of the poles

## Slide 20: FCM reproducibility study

## Slide 21: Towards a quasi-optimum charging time
-4T/h
-3T/h
-1T/h

## Slide 22: Flux creep and flux freezing
Notes: The time dependence of the persistent current in the collective creep model is given by the so-called “interpolation formula”

## Slide 23: Flux creep and flux freezing
µ = 1.1
Notes: The time dependence of the persistent current in the collective creep model is given by the so-called “interpolation formula”

## Slide 24: Flux creep and flux freezing
µ = 6.3
µ = 1.1
Extrapolate to 1 year the field would be around 1.82T
NB: Experiment in preparation to actively stabilise the field amplitude introducing an “acceptable” solenoidal field component.
Notes: The time dependence of the persistent current in the collective creep model is given by the so-called “interpolation formula”

## Slide 25: Summary of the planar staggered array with: 𝜆u=10mm & gap=4.0mm
*The two ATZ samples are not the same thus the one with and the one w/o poles are not directly comparable
Company | RE | type | Undulator field, B (T) |  |  | 𝜎/B
 |  |  | with different pole's material |  |  | 
 |  |  | w/o | FeCo | Ho | 
ATZ | YBCO | TSMG | 1.67* | 1.90 | - | 23%
Nippon | GdBCO | TSMG | - | 2.10 | - | 3%
CAN | GdBCO | TSMG | - | 2.02 | - | 7%
CAN | EuBCO | TSMG | - | 1.90 | - | 6%
CAN | GdBCO | SDMG | 1.69 | 1.89 | 2.01 | 5%
THEVA | GdBCO | tape | 0.78 | 0.88 | - | 8%
SuperOx | YBCO | tape | 0.74 | - | - | 8%

## Slide 26: Summary of the planar staggered array with: 𝜆u=10mm & gap=4.0mm
*The two ATZ samples are not the same thus the one with and the one w/o poles are not directly comparable
Company | RE | type | Undulator field, B (T) |  |  | 𝜎/B
 |  |  | with different pole's material |  |  | 
 |  |  | w/o | FeCo | Ho | 
ATZ | YBCO | TSMG | 1.67* | 1.90 | - | 23%
Nippon | GdBCO | TSMG | - | 2.10 | - | 3%
CAN | GdBCO | TSMG | - | 2.02 | - | 7%
CAN | EuBCO | TSMG | - | 1.90 | - | 6%
CAN | GdBCO | SDMG | 1.69 | 1.89 | 2.01 | 5%
THEVA | GdBCO | tape | 0.78 | 0.88 | - | 8%
SuperOx | YBCO | tape | 0.74 | - | - | 8%

## Slide 27: Summary of the planar staggered array with: 𝜆u=10mm & gap=4.0mm
*The two ATZ samples are not the same thus the one with and the one w/o poles are not directly comparable
Company | RE | type | Undulator field, B (T) |  |  | 𝜎/B
 |  |  | with different pole's material |  |  | 
 |  |  | w/o | FeCo | Ho | 
ATZ | YBCO | TSMG | 1.67* | 1.90 | - | 23%
Nippon | GdBCO | TSMG | - | 2.10 | - | 3%
CAN | GdBCO | TSMG | - | 2.02 | - | 7%
CAN | EuBCO | TSMG | - | 1.90 | - | 6%
CAN | GdBCO | SDMG | 1.69 | 1.89 | 2.01 | 5%
THEVA | GdBCO | tape | 0.78 | 0.88 | - | 8%
SuperOx | YBCO | tape | 0.74 | - | - | 8%

## Slide 28: Summary of the planar staggered array with: 𝜆u=10mm & gap=4.0mm
*The two ATZ samples are not the same thus the one with and the one w/o poles are not directly comparable
†Those are not measurements but just extrapolations
Company | RE | type | Undulator field, B (T) |  |  | 𝜎/B
 |  |  | with different pole's material |  |  | 
 |  |  | w/o | FeCo | Ho | 
ATZ | YBCO | TSMG | 1.67* | 1.90 | - | 23%
Nippon | GdBCO | TSMG | - | 2.10 | 2.20† | 3%
CAN | GdBCO | TSMG | - | 2.02 | 2.12† | 7%
CAN | EuBCO | TSMG | - | 1.90 | 2.00† | 6%
CAN | GdBCO | SDMG | 1.69 | 1.89 | 2.01 | 5%
THEVA | GdBCO | tape | 0.78 | 0.88 | - | 8%
SuperOx | YBCO | tape | 0.74 | - | - | 8%

## Slide 29: Overview
Introduction
Results of the short sample experimental campaign:
  Sample preparation
  Magnetic measurements: Field optimisation, CoFe versus Ho poles, FCM Reproducibility, Charging time, Flux creep & flux freezing
The meter-long prototype
  Design
  Status of the production
Conclusions

## Slide 30
Meter long HTS Insert
Specifications:
active length = 1.0 m
period length = 10.5 mm
total length < 2.0m
period length = 10.5mm
magnetic gap : 4.5mm
B0 ∼ 1.8 T
Cryocoolers
HTS temp 10K
LTS temp 4.0K

## Slide 31
Meter long HTS Insert
1
2
3
4
12T Solenoid
HTS Insert
Cryo 1
Cryo 2a
Cryo 2b
Current leads
Current leads

## Slide 32
Meter long HTS Insert
1
2
3
4
12T Solenoid
HTS Insert
Cryo 1
Cryo 2a
Cryo 2b
Current leads
Current leads

## Slide 33
Meter long HTS Insert
1
2
3
4
12T Solenoid
HTS Insert
Cryo 1
Cryo 2a
Cryo 2b
Current leads
Current leads

## Slide 34
GdBCO-Cu disks (190 pieces) Ho-Cu disks (187 pieces)
Flexor support
Flexor support
Cu-Cooling strap
Meter long HTS Insert
Designed by Mike Giger

## Slide 35
Bulk structure
Flexor support
Cu-Cooling strap
Meter long HTS Insert
Designed by Mike Giger

## Slide 36
Meter long HTS Insert

## Slide 37
Meter long HTS Insert

## Slide 38
Batavia, October 18th 2022

## Slide 39
12T Nb3Sn Solenoid

## Slide 40
12T Nb3Sn Solenoid

## Slide 41
12T Nb3Sn Solenoid

## Slide 42
12T Nb3Sn Solenoid

## Slide 43
12T Nb3Sn Solenoid

## Slide 44
12T Nb3Sn Solenoid

## Slide 45
12T Nb3Sn Solenoid

## Slide 46
12T Nb3Sn Solenoid

## Slide 47
12T Nb3Sn Solenoid
The thermal treatment of two out of four coils has been completed.

## Slide 48
12T Nb3Sn Solenoid

## Slide 49
12T Nb3Sn Solenoid

## Slide 50: Conclusions & Outlooks
We demonstrated high magnetic fields (2T) and algorithms for the optimisation.
Holmium poles deliver higher fields than FeCo even if they are not single crystals.
The reproducibility of the Field Cooling Magnetisation is within our measurement accuracy (0.1%)
A preliminary optimisation of the magnet charging process has reduced the required time from 10 hours to 4 hours.
Flux freezing helps to significantly reduce magnetic creep, although it does not eliminate it completely.
Delivery of the “Cryo-Solenoid” to PSI is expected in Q1 2026, after an intensive measurement campaign will follow, aiming to demonstrate phase errors as low as a few degrees and the device is planned for installation in SLS2.0 in early 2027.

## Slide 51: CAN-SUPERCONDUCTOR: SDMG
Single-direction Melt Growth (SDMG) is a novel approach for REBCO single-domain bulk growth, where a grown bulk from a REBCO system with higher peritectic temperature is used to seed the grown bulk (instead of a NdBCO thin-film seed, which is used for both TSMG and TSIG). The main advantage of this approach is that the bulk is composed exclusively of the c-growth region, unlike TSMG-grown bulks. Therefore, the expected homogeneity is significantly higher in SDMG-grown bulks, as no growth interfaces are present in the bulks.
Courtesy of Dr Tomáš Hlásek (CAN)

## Slide 52: CAN / SDMG + Ho poles